## Slide 1
2018 ROUND ROBIN EXERCISE Thermally altered coals
Convenors:
Dr. Jolanta Kus Dr. Magdalena Misz-Kennan
Dr. Deolinda Flores
Geochemistry of Oil and Coal (B 1.5)
Federal Institute for Geosciences and Natural Resources
Stilleweg 2
D-30655 Hannover
Germany
e-mail: J.Kus@bgr.de
ICCP COMMISSION III
Self-Heating WG

## Slide 2
Photo 1.0
Vitrinite reflectance: 0.96% VRr; NA% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 3
Photo 2.0
Vitrinite reflectance: 0.96% VRr; NA% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 4
Photo 3.0
Vitrinite reflectance: 0.96% VRr; NA% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 5
Photo 4.0
Vitrinite reflectance: 1.53% VRr; NA% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 6
Photo 5.0
Vitrinite reflectance: 1.53% VRr; NA% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 7
Photo 6.0
Vitrinite reflectance: 0.94% VRr; NA% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 8
Photo 7.0
Vitrinite reflectance: 0.94% VRr; NA% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 9
Photo 8.0
Vitrinite reflectance: 1.28% VRr; NA% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 10
Photo 9.0
Vitrinite reflectance: 1.28% VRr; NA% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 11
Photo 10.0
Vitrinite reflectance: 1.28% VRr; NA% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 12
Photo 11.0
Vitrinite reflectance: 0.92% VRr; NA% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 13
Photo 12.0
Vitrinite reflectance: 0.92% VRr; NA% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 14
Photo 13.0
Vitrinite reflectance: 0.92% VRr; NA% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 15
Photo 14.0
Vitrinite reflectance: 0.93% VRr; NA% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 16
Photo 15.0
Vitrinite reflectance: 0.93% VRr; NA% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 17
Photo 16.0
Vitrinite reflectance: 0.96% VRr; NA% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 18
Photo 17.0
Vitrinite reflectance: 1.01% VRr; NA% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 19
Photo 18.0
Vitrinite reflectance: 1.30% VRr; 1.43% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 20
Photo 19.0
Vitrinite reflectance: 1.39% VRr; 1.49% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 21
Photo 20.0
Vitrinite reflectance: 1.39% VRr; 1.49% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 22
Photo 21.0
Vitrinite reflectance: 1.49% VRr; 1.58% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 23
Photo 22.0
Vitrinite reflectance: 1.49% VRr; 1.58% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 24
Photo 23.0
Vitrinite reflectance: 0.93% VRr; 1.05% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 25
Photo 24.0
Vitrinite reflectance: 0.92% VRr; 1.01% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 26
Photo 25.0
Vitrinite reflectance: 0.92% VRr; 1.01% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 27
Photo 26.0
Vitrinite reflectance: 0.92% VRr; 0.99% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 28
Photo 27.0
Vitrinite reflectance: 1.13% VRr; 1.20% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 29
Photo 28.0
Vitrinite reflectance: 1.13% VRr; 1.20% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 30
Photo 29.0
Vitrinite reflectance: 1.13% VRr; 1.20% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 31
Photo 30.0
Vitrinite reflectance: 4.40% VRr; 2.93% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 32
Photo 31.0
Vitrinite reflectance: 4.40% VRr; 2.93% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 33
Photo 32.0
Vitrinite reflectance: 5.16% VRr; 5.32% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 34
Photo 33.0
Vitrinite reflectance: 1.60% VRr; 1.71% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 35
Photo 34.0
Vitrinite reflectance: 1.60% VRr; 1.72% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 36
Photo 35.0
Vitrinite reflectance: 1.60% VRr; 1.72% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 37
Photo 36.0
Vitrinite reflectance: 1.62% VRr; 1.72% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 38
Photo 37.0
Vitrinite reflectance: 1.80% VRr; 1.96% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 39
Photo 38.0
Vitrinite reflectance: 2.01% VRr; 2.09% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 40
Photo 39.0
Vitrinite reflectance: 4.40% VRr; 2.93% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 41
Photo 40.0
Vitrinite reflectance: 4.40% VRr; 2.93% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 42
Photo 41.0
Vitrinite reflectance: 4.40% VRr; 2.93% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 43
Photo 42.0
Vitrinite reflectance: 1.40% VRr; 1.48% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 44
Photo 43.0
Vitrinite reflectance: 1.40% VRr; 1.48% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 45
Photo 44.0
Vitrinite reflectance: 1.40% VRr; 1.48% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 46
Photo 45.0
Vitrinite reflectance: 1.40% VRr; 1.48% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 47
Photo 46.0
Vitrinite reflectance: 1.13% VRr; 1.20% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 48
Photo 47.0
Vitrinite reflectance: 1.13% VRr; 1.20% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 49
Photo 48.0
Vitrinite reflectance: 1.13% VRr; 1.20% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 50
Photo 49.0
Vitrinite reflectance: 4.40% VRr; 2.93% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 51
Photo 50.0
Vitrinite reflectance: 4.40% VRr; 2.93% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 52
Photo 51.0
Vitrinite reflectance: 4.40% VRr; 2.93% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 53
Photo 52.0
Vitrinite reflectance: 4.40% VRr; 2.93% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 54
Photo 53.0
Vitrinite reflectance: 4.40% VRr; 2.93% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 55
Photo 54.0
Vitrinite reflectance: 4.40% VRr; 2.93% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 56
Photo 55.0
Vitrinite reflectance: 0.82% VRr; NA% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 57
Photo 56.0
Vitrinite reflectance: 0.82% VRr; NA% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 58
Photo 57.0
Vitrinite reflectance: 1.63% VRr; 1.66% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 59
Photo 58.0
Vitrinite reflectance: 2.01% VRr; 2.09% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 60
Photo 59.1
Vitrinite reflectance: 1.93% VRr; 2.00% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 61
Photo 59.2
Vitrinite reflectance: 1.93% VRr; 2.00% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 62
Photo 60.1
Vitrinite reflectance: 1.93% VRr; 2.00% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.

## Slide 63
Photo 60.2
Vitrinite reflectance: 1.93% VRr; 2.00% VRmax
Reflectance values below 0.90% VRr and above 0.98 VRr are considered to
be oxidatively and thermally altered.